Taralay Premium Comfort

TARALAY PREMIUM COMFORT is a multilayered calendered and pressed acoustic PVC floorcovering available in 2m wide sheet (Group T wear rating).

The product comprises a ≥ 1mm thick, pure, PVC wearlayer incorporating very densely pressed coloured chips, and a Very High Density (VHD) foam (yielding a 16 dB sound insulation rating) reinforced with a glass fibre grid.

TARALAY PREMIUM COMFORT’s calendered wearlayer is treated with Protecsol®, a UV cured anti-glazing surface treatment to facilitate easy maintenance and permanently eliminates the need for acrylic emulsion (metallisation).

The product is antistatic (AS class 1) and incorporates Sanosol®, an anti-bacterial and fungicidal treatment.