DECOFRESC

# DECOFRESC

Protection and decorative frescoes - All public contemporary or early childhood

Description: wall protection and decoration panel (Cloud or Wave Decofresc –All public contemporary– or Savannah, Maritime, Altitude Decofresc –Early childhood- as manufactured by Gerflor) from rigid and antibacterial PVC achieving Bs2d0 fire rating with solid colour and textured surface. 3 m long, 1.30 m wide (indivisible), 2 mm thick.

No heavy metals and no substance potentially subjected to any REACH restriction are used in its manufacture. The calcium-zinc thermal stabilisation process is used. The emission level of volatile substance in inside air has been tested according to ISO 16000 and is under 15μg/m3.100% of the product are recyclable.

Colour: selected by architects from manufacturer’s standard range.

Installation sequence: glue as per manufacturer’s instructions.