DECOPRINT

# DECOPRINT

# Protection panel with customised digital printing

Description protection panel with customized digital printing (Decoprint as manufactured by Gerflor) from translucent antibacterial PVC achieving Bs2d0 fire rating with images printed on the back. The surface is lightly textured. Its maximum height is 1.20 m and its maximum length is 2.90 m and 1 mm thick

No heavy metals and no substance potentially subjected to any REACH restriction are used in its manufacture. The calcium-zinc thermal stabilisation process is used. The emission level of volatile substance in inside air has been tested according to ISO 16000 and is under 15μg/m3.100% of the product are recyclable.

Colour: customized and selected by architects.

Installation sequence: glue as per manufacturer’s instructions.